Flamex® One

Fire rated, one-component, acrylic joint sealant for internal joints

* 1. **Fire Rated Sealant**
	2. Where indicated on the drawings, joints shall be sealed with an acrylic sealant capable of fire resistance up to 4 hours according to AS1530.4:2014.
	3. The fire rated sealant will be installed in a configuration (joint width / joint depth) which provides the joint with (*specify*) hours fire rating. (*refer to the current TDS for FRL details*)
	4. The fire rated sealant will be capable of accommodating +/-10% joint movement (20% total)
	5. **Fosroc Flamex One** meets the performance criteria and approved for this application.