Vandex Plug

**Cementitious plugging mortar.**

**1.00 Leak plugging**

Where required, concrete and masonry surfaces subject to water leakage are to have the water leaks identified and repaired, using a rapid setting, cementitious plugging mortar.

**1.10 Surface Preparation**

 All cracks and leakage points are to be chiselled out to create a rebate, having a minimum width and depth of 25mm.

**1.20 Plugging material**

 The plugging material is to consist of cement powder, graded quartz sands and inorganic additives, generally mixed on site with water and applied as a putty by hand or spatula into the repair (refer to the product TDS).

 It shall exhibit the following properties:

|  |  |
| --- | --- |
| **Colour:** | Grey |
| **Bulk density:** | 1.10 – 1.30 kg / L |
| **Initial setting time:** | 30 seconds after mixing with water @ 20oC |
| **Application temperature:** | 5 – 30oC |

**1.30** **Vandex Plug** meets the performance criteria and is approved.

Mar-07

Mar-07